## Slide 1: MEASUREMENT of FRICTION PROPERTIES

## Slide 2: MEASUREMENT APPROACH
Scientific / Design /Engineering:
  Available Force from Macro-texture Component
    Measure macro-texture
  Available Force from Micro-texture Component
    Measure micro-texture
Practical:
  Combined Vehicle Control Force
  Measure Macro-texture

## Slide 3: CURRENT MD METHOD
E-274 Skid Truck
  Measures Drag Force during Sliding Friction
  Primary Sensor – Tire (grooved - smooth)
  Collect Average value over 59 ft.*
  Total Test Sequence ~ 225 ft.*
  Water consumed - ~ 2 gal.
* = at 40 mph

## Slide 4: TYPICAL EQUIPMENT

## Slide 5: ATYPICAL EQUIPMENT

## Slide 6: TYPICAL TEST

## Slide 7: CURRENT APPLICATION
Test network every 1056 ft. if > 1 mi
Test every 528 ft. if < 1 mi.
Deemed not testable if < ¼ mile
Ribbed tire – focus on micro-texture
Test driver’s side wheel-path
Test at Speed Limit with 40 mph Maximum
Adjust Collected Value by - 0.6 SN per MPH
  (true adjustment is dependent on surface properties)

## Slide 8: ISSUES
Sampling 6% - 10% of pavement
Large sample spacing:
  Water consumption
  Total test sequence time
  Lost tests at intersections etc.
Measuring “locked” friction
Test spacing too far for ramps etc.

## Slide 9: WHY
Miss key pavement sections of concern:
  Ramps, Sharp curves, Traffic control areas
  Sections shorter that ¼ mile very difficult to test
Apply the limited sample resources more effectively
Increase the size of the sample (moderate)
Functional test should more closely resemble the typical vehicle application

## Slide 10: LIMITATIONS
PRIMARY:
  Water ……. 400-1000 gallons
  Tire Tread …… 1/8 inch
SECONDARY:
  Braking Energy
  Mechanical System Speeds

## Slide 11: SCRATCH SYSTEM
Tire Tread Width – 4” (narrower tire)
Water consumption - ~ 0.2 gals/ test
Down Force – 675 pounds (lighter trailer)
One Second Total Test Cycle
Digital Reliability Everywhere Possible
Include:
  Macro-texture Measurement
  Sub-meter GPS

## Slide 12: E-274 BASED PROPOSAL
Data averaging time of 0.1 to 0.2 sec (6-12ft.)
Start averaging at 60% - 80% “lock-up”
Reduce total test time to 1 – 1.5 sec
Reduce water consumption to ~ 0.5 gal
Routine sample spacing - 0.05 mi (264ft)
Short routes and projects - 0.02 mi. (105 ft)

## Slide 13: IMMEDIATE ACTIONS
Purchase a more flexible device – July 2013
  Flexible control software:
    Change test timing (percent slip, time)
    Data sample rate ?
  Improve water control:
    Rapid electric flow control
    Small accumulator for shock control ?
  Improve data processing for the increased rate
    Low noise, functional filtering
  Include macro-texture laser and GPS

## Slide 14: POTENTIAL FUTURE ACTIONS
Servo driven water pump system on the trailer*
More robust braking system with sturdier axles*
Narrower test tire (full diameter) with a narrower nozzle to further reduce water requirements by ~30%
  *May be included in current device as vendor option

## Slide 15: QUESTIONS?