## Slide 1: COMPARISON OF MPD VALUES FROM HIGH-SPEED LASER MEASUREMENTS WITH MPD FROM TWO STATIONARY DEVICES
Rohan Perera, PhD, PE
Soil and Materials Engineers, Inc.
Plymouth, Michigan
Larry Wiser
Federal Highway Administration
McLean, VA
RPUG 2013, San Antonio, TX

## Slide 2: Pavement Texture (ISO)

## Slide 3: Macrotexture
Friction.
Tire Pavement Noise.
Rolling Resistance.

## Slide 4: Measurement of Macrotexture
ASTM E 965, Sand Patch Test, Mean Texture Depth (MTD).
ASTM E 1845, Laser Measurements, Mean Profile Depth (MPD).
ASTM E 1845 has a regression equation to estimate MTD from MPD.

## Slide 5: Measurement of Macrotexture at Network Level
Single point laser sensor installed on a vehicle. Compute MPD from collected data.
Simulate a digital sand patch on 3D data (e.g., Pavemetrics LCMS Data).

## Slide 6: Computation of MPD, ASTM E 1845
Baseline = 100 mm
= 100 mm

## Slide 7: LTPP Profilers - 2013
Texture Lasers: LMI Selcom Optocator 2008-180/390, 62.5 kHz

## Slide 8: LMI Optocator 2008
From LMI-Selcom User Manual

## Slide 9: Capabilities of Texture Laser
Data are sampled at 62.5 kHz and all collected data are saved.
For LTPP purposes data are decimated to obtain data at 0.5 mm intervals.

## Slide 10: Data Collected at Concrete Section
Transverse Tines

## Slide 11: Checking Accuracy of Texture Laser
Block check.
Texture Reference Disk provided by Ames Engineering.

## Slide 12: Block Check

## Slide 13: Texture Reference Disk
Machined hard disk with four steps alternating from 0.5 to 1.0 mm.

## Slide 14: Texture Reference Disk
Disk attains a speed of 7200 rpm and starts taking measurements. Simulates a speed of 54 mph.
MPD computed from data displayed on the computer.
Theoretical MPD of Disk = 0.75 mm.
Collected data can also be viewed.

## Slide 15
Comparison of MPD From High-Speed Device with MPD From CT Meter and Ames Scanner

## Slide 16: CT Meter
Sensor mounted on a rotating arm.
Follows a circular path having a radius of 142 mm.
Sample spacing = 0.87 mm.

## Slide 17: MPD From CT Meter – Repeatability Asphalt Section

## Slide 18: CT Meter - MPD on Asphalt Section at 2 m Intervals Along Right Wheelpath

## Slide 19: Ames Engineering Scanner
Dimensions: (Width, Height, Depth) 6” x 9” x 6”.
Laser travels 100 mm along a longitudinal path.
Was set to get 10 scans over a 75 mm width.
Sample spacing approx. 0.014 mm.

## Slide 20: Analysis Procedure
Three Test Sections: Two asphalt (AC-1, AC-2), and one chip seal (CS).
CT Meter and Ames Scanner tests performed over a 10 m distance at 2 m intervals. Results averaged.
Average MPD from macrotexture data collected by high-speed device computed over same 10 m distance.

## Slide 21: Test Section AC-1, Dense-Graded AC

## Slide 22: Test Section AC-2, Dense-Graded AC

## Slide 23: Test Section – Chip Seal

## Slide 24: Repeatability of MPD from High-Speed Device Over 10 m

## Slide 25: Comparison of MPD Values

## Slide 26: Comparison of MPD Values

## Slide 27: Issues
Improved procedures for verifying accuracy of macrotexture data collected by high-speed devices is necessary.
High-frequency laser sensors may be noisy, thereby affecting MPD values.
Single spikes were noted in the macrotexture data. Robust spike detection algorithms are needed.

## Slide 28: Issues
ASTM E 1845 specifies a low-pass filter to be applied on the data before computing MPD. Differences on how the low-pass filter is programmed can affect MPD values.
Need for a “standard” program to check MPD computations
Data from high-speed laser is time-based. Lower speeds means more data are collected. Speed may affect MPD.
Outlier detection scheme is needed to avoid cracks affecting MPD values.