## Slide 1: Use Ground Penetrating Radar Technology to Evaluate Rutting in An Asphalt Overlay
Feng Hong, PE, PhD, TxDOT
Darhao Chen, PE, PhD, TxDOT
September 16~19, 2013, RPUG Meeting, San Antonio, TX

## Slide 2: Table of Contents
4-6
7
8-16
17-18
19
3
Introduction
Background
Experimental Design
Nondestructive Testing with GPR
Trench Verification
Conclusion Remarks
1
2
3
4
5
6

## Slide 3: Introduction
What is rut
Causes of rut
Layer-based rut study
Methods to evaluate layer-based rut
Focus of this study

## Slide 4: Background (1)
Pavement structure
Hot rubber seal: 2006
Hot mix asphalt overlay: 1998
Project history
~2” TyC HMA
~4~5” TyB HMA
~8” CRC
~6” CTB
Subgrade
Hot rubber seal
Seal coat
Fabric underseal
Traffic
2010 AADT: 24610
Truck percentage: 26%
20 years ESALs: 33 million

## Slide 5: Background (2)

## Slide 6: Background (3)

## Slide 7: Experimental Design
NDT and DT complement each other to accommodate evaluation of permanent deformation across the entire length of the segment under study.
Ground Penetrating Radar used to estimate pavement layer thickness
  Right wheel path
  Middle of lane
Coring used to calibrate GPR thickness estimates
Trenching used to verify permanent deformation estimated by GPR
Non destructive testing
Destructive testing

## Slide 8: GPR Principle
Pavement

## Slide 9: GPR Colorful Map View

## Slide 10: Thickness Estimation Based on GPR Signal
A1: Amplitude of reflection from pavement surface, in volt;
Am: Amplitude of reflection from a metal plate (placed on a pavement surface), in volt.
c: A constant representing the speed of the EM wave traveling in the air, i.e. approximately 3x108 m/s or 11.8 inch/ns; and
t: One way travel time of an EM wave in a given layer.
Dielectric
Thickness

## Slide 11: Total AC Overlay Thickness
Middle of Lane
Right Wheel Path

## Slide 12: AC Layer Thickness Along Different Scan Lines
Right Wheel Path
Middle of Lane

## Slide 13: Thickness Calibration

## Slide 14: Calibration Results

## Slide 15: Layer Based Thickness Comparison
AC Layer 1
AC Layer 2

## Slide 16: Layer Based Permanent Deformation Statistics

## Slide 17: Trenching in Field

## Slide 18: Permanent Deformation from Trench
PD (in.) | GPR | Trench
Layer 1 | 0.63 | 0.63
Layer 2 | 0.27 | 0.38

## Slide 19: Conclusion Remarks
GPR can serve as an effective tool to
  Evaluate permanent deformation in AC overlay
  Identify layer-based permanent deformation
  Provide full length survey coverage
  Provide fast and nondestructive survey results

## Slide 20: Thank You & Be Safe